| 助成番号 ０６０５３８ |  | ６－２ |
| --- | --- | --- |

研 究 成 果 報 告 書

（国立情報学研究所の民間助成研究成果概要データベース・登録原稿）

| 研究テーマ （和文） ＡＢ | 自己組織化を利用したスピンクロスオーバー錯体薄膜の作製と評価 |
| --- | --- |
| 研究テーマ （欧文） ＡＺ |  |
| 研 究氏 代 表名 者 | ｶﾀｶﾅ ＣＣ | 姓）マツダ | 名）マサキ | 研究期間 Ｂ | １８ ～ ２０ 年 |
|  | 漢字 ＣＢ | 松田 | 真生 | 報告年度 ＹR | ２０ 年 |
|  | ﾛｰﾏ字 ＣＺ | MATSUDA | MASAKI | 研究機関名 | 東京大学 |
| 研究代表者 ＣＤ 所属機関・職名 | 東京大学物性研究所 助教 |
| 概要 ＥＡ (600字～800字程度にまとめてください。) 交互積層法を利用して自己組織的に基板上にスピンクロスオーバー錯体を作製するために、アンカーとブリッジとなるべき配位子のデザインと合成を試みた。高温領域でスピン転移が確認されている、pyrazolやbenzimidazolを利用すべく実験を行ったが、目的に沿う分子の合成には至っていない。 一方で、2,6-di(pyrazol-1-yl)pyridine（以下、dppと略す）からなる[Fe(dpp)2](BF4)2錯体は、極性溶媒に可溶なうえに溶液中でのスピン転移も報告されており[1]、この錯体ならば単純なスピンコート法による薄膜化が可能であると予想した。文献に従い合成を行って得られた黄色い錯体のアセトニトリル溶液をガラス基板にスピンコートしたところ、平滑な黄色い薄膜を得ることが出来た。得られた薄膜の磁化の温度依存性を測定すると、バルク結晶と同様に260 K付近でスピン転移を観測でき、スピンクロスオーバー錯体の薄膜作製に成功していることが確認された。 さらに、この薄膜を有機EL素子の活性層に導入することを試みた。スピン転移に伴うＥＬ素子の特性変調が期待できる。発光物質としてchlorophyll aを用い、活性層を[Fe(dpp)2](BF4)2との混合膜にしたITO/chlorophyll a : [Fe(dpp)2](BF4)2 / Al構造の素子を作製したところ、300 Kではchlorophyll aに由来した発光が明確に観測されたものの、200 Kではそれが消光する現象を見いだした。ELスペクトルの温度依存性から、発光の消失は260 K付近で起こっており、chlorophyll a のみで作製した参照素子では200 Kでも明確に発光が観測されることから、[Fe(dpp)2](BF4)2を導入した素子においてはそのスピン転移によって発光のON/OFF状態をスイッチング出来ていることが分かった。このような現象は本研究において初めて見いだされたものである。 [1] J. M. Holland et al, J. Chem. Soc., Dalton Trans. 2002, 548. |
| キーワード ＦＡ | スピンクロスオーバー錯体 | スピン転移 | 薄膜 | 有機EL |

（以下は記入しないでください。）

| 助成財団ｺｰﾄﾞ ＴＡ |  |  |  |  | 研究課題番号 ＡＡ |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 研究機関番号 ＡＣ |  |  |  |  |  | シート番号 |  |

| 発表文献（この研究を発表した雑誌・図書について記入してください。） |
| --- |
| 雑 誌 | 論文標題ＧＢ | Thin film of a spin crossover complex [Fe(dpp)2](BF4)2 |
|  | 著者名 ＧＡ | M. Matsuda and H. Tajima | 雑誌名 ＧＣ | Chemistry Letters |
|  | ページ ＧＦ | 700～701 | 発行年 ＧＥ | 2 | 0 | 0 | 7 | 巻号 ＧＤ | 36 |
| 雑 誌 | 論文標題ＧＢ | Electroluminescence quenching caused by a spin crossover transition |
|  | 著者名 ＧＡ | M. Matsuda, H. Isozaki and H. Tajima | 雑誌名 ＧＣ | Chemistry Letters |
|  | ページ ＧＦ | 374～375 | 発行年 ＧＥ | 2 | 0 | 0 | 8 | 巻号 ＧＤ | 37 |
| 雑 誌 | 論文標題ＧＢ | Reproducible on-off switching of the light emission from electroluminescence device containing a spin crossover complex |
|  | 著者名 ＧＡ | M. Matsuda, H. Isozaki and H. Tajima | 雑誌名 ＧＣ | Thin Solid Films |
|  | ページ ＧＦ | ～ | 発行年 ＧＥ |  |  |  |  | 巻号 ＧＤ | 印刷中 |
| 図 書 | 著者名 ＨＡ |  |
|  | 書名 ＨＣ |  |
|  | 出版者 ＨＢ |  | 発行年 ＨＤ |  |  |  |  | 総ﾍﾟｰｼﾞ ＨＥ |  |
| 図 書 | 著者名 ＨＡ |  |
|  | 書名 ＨＣ |  |
|  | 出版者 ＨＢ |  | 発行年 ＨＤ |  |  |  |  | 総ﾍﾟｰｼﾞ ＨＥ |  |

欧文概要 ＥＺ In order to fabricate a spin crossover complex film by using the layer-by-layer assembly method, I have tried to synthesize “anchor”and “bridge”molecules, especially based on pyrazol and benzimidazol. However, unfortunately, I have not succeeded in synthesize such molecules. On the other hand, it is reported that a spin crossover complex of [Fe(dpp)2](BF4)2 can be soluble to common polar solvents and the complex shows the spin transition even in the solution state [1]. Thus I expected that it is possible to fabricate a thin film of the spin crossover complex of [Fe(dpp)2](BF4)2 by a simple spin-coating method. The complex was synthesized by procedures described literature, then complex was spin coated on the glass substrate. The AFM measurement revealed that the roughness of the obtained film was low. Furthermore, the temperature dependence of the magnetization of the obtained thin film shows the spin transition around 260 K, that was almost the same to that reported for the bulk crystals of [Fe(dpp)2](BF4)2. This result means that, as expected, the fabrication of a spin crossover complex film is achieved by the simple spin-coating method. I have also tried to introduce the spin crossover complex into the active layer of an organic electroluminescence device, since I expected that it is possible to utilize the spin crossover complex as a component for controlling the properties of organic thin film devices. The configuration of fabricated EL device was ITO / chlorophyll a : [Fe(dpp)2](BF4)2 / Al. From the fabricated device, the EL spectrum of chlorophyll a was clearly observed at 300 K, while it could not be observed at 200 K. The temperature dependence measurement of the EL emission revealed that the EL emission quenches at around 260 K, that is almost the same to the spin transition temperature. The reference device without [Fe(dpp)2](BF4)2 complex shows the EL emission of chlorophyll a even at 200 K. These results strongly suggest that the ON-OFF switching of the EL emission was caused by the spin transition of [Fe(dpp)2](BF4)2. This is a first report of the utilization of the spin crossover complex as a component for controlling the properties of organic thin film device. [1] J. M. Holland et al, J. Chem. Soc., Dalton Trans. 2002, 548.