| 助成番号 060800 |  | ６－２ |
| --- | --- | --- |

研 究 成 果 報 告 書

（国立情報学研究所の民間助成研究成果概要データベース・登録原稿）

| 研究テーマ （和文） ＡＢ | チタニア被覆孤立共役系炭素ポリマーの開発とその物性評価 |
| --- | --- |
| 研究テーマ （欧文） ＡＺ | Preparation and Application of Highly Dispersed Conjugated Polymers / TiO2 Hybrid Materials |
| 研 究氏 代 表名 者 | ｶﾀｶﾅ ＣＣ | 姓） ムラカミ | 名） ヒロト | 研究期間 Ｂ | ２００６ ～ ２００８ 年 |
|  | 漢字 ＣＢ | 村 上 | 裕 人 | 報告年度 ＹR | ２００８年 |
|  | ﾛｰﾏ字 ＣＺ | MURAKAMI | HIROTO | 研究機関名 | 長崎大学 |
| 研究代表者 ＣＤ 所属機関・職名 | 長崎大学大学院生産科学研究科・准教授 |
| 概要 ＥＡ (600字～800字程度にまとめてください。) チタニアと共役系炭素ポリマーの複合材料は、両者の特異な電気的性質のため電子材料としての応用が期待されている。また、共役系炭素ポリマーを孤立分散できれば、複合材料のさらなる性質向上が期待できる。本研究は、孤立共役系炭素ポリマーをチタニアで被覆した複合材料を開発し、その物性評価を行うことを目的とした。本報告では、本研究目的の基礎的知見として、カチオン性基を側鎖に持つ共役炭素ポリマーとアニオン性のポリ酸塩の複合化、およびそのスペクトル評価について述べる。 本研究では、側鎖にカチオン性基を持つポリマーを選んだ。多くの金属酸化物がアニオン性を示すため、対イオンとして金属酸化物を導入しやすいと考えたためである。また、側鎖が多電荷になることでポリマー間の静電反発が誘起され、共役炭素ポリマーが水中で孤立できると考えた。 1,4-bis(2-(diethylmetylammonio)ethoxy)-2,5-diiodobenzeneと1,4-bis(2-(diethylmetylammonio)ethoxy)-2,5- diethynylbenzeneを既知の方法で合成した後、薗頭－荻原カップリング反応によりカチオン性共役炭素ポリマー(1)を合成した。また、既知の方法に従い代表的なポリ酸塩であるポリオキソモデレート錯体([n-C4H9)4N]2[Mo6O19])(2)を合成した。同定は1H-NMRスペクトル測定、MALDI-TOF-MSスペクトル測定を行い目的物であると判断した。 ポリマー1水溶液は412nmに極大吸収を示した。ポリマー1の濃度を増加させても極大吸収波長に変化がなく、吸光度が濃度に比例して増加したことから、ポリマー1が水中で孤立分散していることが分かった。ポリマー1の水溶液にポリ酸塩2の水溶液を加えると、400 nmに新しい極大吸収が現れた。これは、静電的相互作用によってポリマー1とポリ酸塩2の複合体が形成したためである。また、ポリマー1の蛍光スペクトルは加えたポリ酸塩の量の増加に応じて強度が減少した。このことは、電子供与体であるポリマー1から電子受容体であるポリ酸塩2への電子移動を示唆する。ポリマー1水溶液にカチオン性の電子受容体であるメチルビオローゲンを加えても、ポリマー1の吸収スペクトルおよび蛍光スペクトルに変化がなかった。これは、電荷の反発によりビオロゲンがポリマー1に近づけなかったためである。このことからも、ポリマー1とポリ酸塩2の複合体形成が示唆される。 |
| キーワード ＦＡ | 共役炭素ポリマー | ポリ酸塩 | 有機・無機複合材料 | 分子間電子移動 |

（以下は記入しないでください。）

| 助成財団ｺｰﾄﾞ ＴＡ |  |  |  |  | 研究課題番号 ＡＡ |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 研究機関番号 ＡＣ |  |  |  |  |  | シート番号 |  |

| 発表文献（この研究を発表した雑誌・図書について記入してください。） |
| --- |
| 雑 誌 | 論文標題ＧＢ |  |
|  | 著者名 ＧＡ |  | 雑誌名 ＧＣ |  |
|  | ページ ＧＦ | ～ | 発行年 ＧＥ |  |  |  |  | 巻号 ＧＤ |  |
| 雑 誌 | 論文標題ＧＢ |  |
|  | 著者名 ＧＡ |  | 雑誌名 ＧＣ |  |
|  | ページ ＧＦ | ～ | 発行年 ＧＥ |  |  |  |  | 巻号 ＧＤ |  |
| 雑 誌 | 論文標題ＧＢ |  |
|  | 著者名 ＧＡ |  | 雑誌名 ＧＣ |  |
|  | ページ ＧＦ | ～ | 発行年 ＧＥ |  |  |  |  | 巻号 ＧＤ |  |
| 図 書 | 著者名 ＨＡ |  |
|  | 書名 ＨＣ |  |
|  | 出版者 ＨＢ |  | 発行年 ＨＤ |  |  |  |  | 総ﾍﾟｰｼﾞ ＨＥ |  |
| 図 書 | 著者名 ＨＡ |  |
|  | 書名 ＨＣ |  |
|  | 出版者 ＨＢ |  | 発行年 ＨＤ |  |  |  |  | 総ﾍﾟｰｼﾞ ＨＥ |  |

欧文概要 ＥＺ Much attention has been focused on hybrid materials of a conjugated polymer and titania because of their unique electric properties. Our purpose is development of an individually dispersed conjugated polymer coated with titania. Using of the individually dispersed conjugated polymer would make possible to prepare a organic-inorganic hybrid material with hierarchical structure. We describe here the preparation of a hybrid material of a cationic conjugated polymer and anionic polyoxometalate, and its spectral behavior. 1,4-bis(2-(diethylmetylammonio)ethoxy)-2,5-diiodobenzene and 1,4-bis(2-(diethylmetylammonio)ethoxy)-2,5- diethynylbenzene were prepared according to the literature. Both the compounds were treated by Sonogashira-Ogiwara coupling reaction to obtain the polymer (1). Polyoxymolybdate (2), one of the typilcal polyoxometalate, was also prepared according to the literature. Absorption maximum of an aqueous solution of 1 was observed at 412 nm. Absorbance at 412 nm was in proportion to the concentration of 1, indicating individual dispersion of 1 in water. Addition of 2 to the 1 solution resulted in the appearance of new absorption at 400 nm. This is probably due to the formation of the hybrid of 1 and 2. Fluorescence of 1 in water was also quenched by the addition of 2, suggestion electron transfer from excited 1 as an electron donor to 2 as an electron acceptor. Interestingly, the absorption and fluorescence spectra of 1 in water remained the same even thought methylviologen, a cationic electron acceptor, was added to the solution. This is because methylviologen is unable to come close to 1 due to electrostatin repulsion.